## Slide 1: CASS and other Accelerated Corrosion Tests
Presented to the SFEA Surface Finishers Educational Association, Orange County, CA
By: Frank Altmayer, MSF, AESF Fellow, Technical Education Director,
AESF Foundation/NASF

## Slide 2: Common Corrosion Mechanisms
Chemical attack
Bi-metallic (aka galvanic)
Oxygen concentration cell
  Crevice corrosion
  Poultice corrosion
  Filiform corrosion
Fretting Corrosion
Stress corrosion
Automobile Body
Hydraulic Shaft

## Slide 3: Accelerated Corrosion Tests
*Note: Exposure times for automotive specifications covering Cu/Ni/Cr over plastics typically are 60-80hrs
Test | ASTM | Coating | Typical Hrs. | Mechanism | Service
Salt Spray | B117 | Various | 8-2000 | O2 Cell | Outdoors: moderate to severe exposures
CASS | B368 | Cu/Ni/Cr Ni/Cr | 44 (SC5) 22 (SC4)* | O2 Cell + galvanic + mild acid attack | moderate to severe, parts not subject to dirt accumulation
Corrodkote | B380 | Cu/Ni/Cr Ni/Cr | 3-24hr cycles | O2 Cell + galvanic | moderate to severe, parts subjected to dirt accumulation
Russian Mud | B995 | Cu/Ni/Cr Ni/Cr | 48-168 | O2 Cell + galvanic | moderate to severe, parts subjected to dirt accumulation
AASS | G85 | Various | 8-2000 | O2 Cell + Acid attack | Moderate, parts not subject to dirt accumulation
Kesternich | B605 | Sn/Ni, stable coatings | 24 hr. | O2 Cell + Severe acid Attack | Industrial, highly stable coatings

## Slide 4
Background:
Russians love cars with decorative chromium
2006-7, Winter in Moscow was very cold with lots of snow
City crews changed to calcium chloride for street de-icing
Decorative Cr on new cars corroded in just a few winter months
Why Calcium Chloride vs. NaCl?
Melts ice 8 times faster
Works down to -25ºF (exothermic reaction) vs. 12ºF for NaCl
Does not form dust
Can be applied before a storm
Russian Mud???
Winter in Moscow, 2006-7
Photo, courtesy of Don Snyder, Atotech USA

## Slide 5: Ni-Cr Corrosion Protection Options:
Ni Layers | Cr Type | Comments
SBN + BN | Cr+6 or Cr+3 | Outdoor, non-vehicular applications
SBN + HSN + BN + MPN | Cr+6 | Parts perform well in 96 hr. CASS, 480hr. NSS, but poor results in Russian Mud, brake dust exposure
SBN + HSN + BN + MPN or SBN + HSN + BN + NN | Cr+3 | Parts perform well in Russian Mud exposure, but poor results in CASS, NSS and brake dust
SBN + HSN + BN + MPN or MP-EN-P | Cr+3 + Passivate | Parts perform well in Russian Mud exposure, as well as CASS, NSS and when exposed to brake dust
Notes:
Satin nickel can be substituted for bright nickel
Copper can be applied as an under-plate to SBM, but the nickel thickness required is almost the same
Thickness of nickel layers depends on the type of substrate
Recommendations can be found in ASTM B456

## Slide 6: Passivation of Cr+3 Deposits
Options:
Immersion in Cr+3 solution*
Chromium phosphate (CrPO4), g/L: 20-35
Oxalic acid, g/L: 6-12
Phosphoric acid: to pH 1-1.5
Temperature: 35ºC
Time: 5-30 seconds
Cathodic treatment in Cr+3 solution**
Basic chromium sulfate (Cr2(SO4)3, g/L: 10g/L
Sodium gluconate, g/L 3.8g/L
Temperature: 25ºC
pH: 3.5
CCD: 0.5-1.0A/dm2
Time: 40-240 seconds
*per EP3502320A1 **per US10415148

## Slide 7: Introduction
Typical Corrosion Resistance Requirements*
Test | ASTM | Hrs. | Requirement
Neutral Salt Spray | B117 | 480 | No visible change
CASS | B368 | 22-96 | No visible change
CASS (active sites) | B456 X5 | Test is conducted after CASS exposure | 2,000/cm2, active sites should average <0.032mm in diameter, no pit larger than 0.0635mm in diameter
Russian Mud | B995 | Variable | Rating = 5 (No visible change) Rating = 4 (Slight haze/stain no attack on Cr)
* For exterior automotive and motorcycle parts.
Requirements may vary significantly from one manufacturer to another

## Slide 8: The CASS Test, ASTM B368
For decorative electrodeposited coatings
Nickel/chromium coatings
Copper/nickel/chromium coatings
Substrates designed for severe service:
  Steel
  Zinc alloys
  Aluminum alloys
  Plastics
  Others
Also applicable for anodized aluminum
(Copper Accelerated Salt Spray)

## Slide 9
CASS vs. Salt Spray
Operating Parameter | CASS | Salt Spray
Temperature, ºC | 49 +/-1 | 35 +/- 2
Salt Solution | 5% NaCl + 0.25g/L CuCl2 | 5% NaCl
pH | 3.1 to 3.3 | 6.5-7.2
Collection rate | 1-2mL/hr/80cm2 | 1-2mL/hr/80cm2
Verification test panels | Nickel | Steel
Part prep | Cleaning required | Usually not cleaned
Exposure angle* | 15-30º, 180º | 15-30º, 6º
pH Adjust | Acetic/NaOH | HCl/NaOH
Notes:
Equipment used for each test is the same
Do not use one chamber for both tests
* 180º exposure is for automotive parts that are installed in a horizontal orientation, 6º exposure is typically in Boeing/aerospace specifications

## Slide 10
Evaluating CASS Test Specimens
GMW 264 Acceptable (top) and unacceptable (bottom) results
ASTM does not indicate what constitutes a pass or fail for the CASS test, leaving interpretation to the part manufacturer
Requirements vary significantly
Some OEMs require “no change”
Other OEMs may indicate a certain number of corrosion spots, none larger than a specific diameter
Another criteria that may be used is the number of “active” corrosion sites detected after exposure

## Slide 11
Principle:
“Active” sites per unit area may more closely match CASS performance in tests longer than 24 hrs.
Procedure:
Subject part to “normal” CASS exposure
Rinse, dry the part
Strip chromium deposit (ASTM provides no guidance on stripping method)
Using a microscope at 100-200X, count the “active” sites
  Active sites are typically larger and have a darker/rougher texture
  Average diameter should be <0.032mm, largest pore should not be >0.0635mm in diameter
Acceptable active pore density is determined by each OEM
  GM 4372/73/74M require a minimum of 2,000 active pores/cm2
Determination of “Active” Pore Density
Active pore charts from GM4372-3-4M
2,000/cm2
10,000/cm2

## Slide 12
Use 4 nickel panels (specification B162, <0.15% C)
  10 X 7.5 cm, approximately 0.09 cm thick
  Weigh each panel on an analytical balance (to 0.001g)
  Using plastic supports, place one panel at 30° from vertical, in each corner of chamber
  Panels should be on the inboard side of condensate collectors, parallel to the cabinet length
  The top of the test panels should be at the same height as the top of the condensate collectors
Calibrating & Standardizing Corrosive Conditions Within Cabinet
30°

## Slide 13
After 22 hour exposure:
  Rinse panels in DI water
  Immerse in 20%vol HCl @20-25°C, for 2 minutes
  Handle panels with (preferably) non-metallic tongs
  Rinse in room temperature water
  Rinse again in warm 38°C flowing water
  Dry panels in 100°C oven for 10 minutes
  Cool to room temperature (preferably in a desiccator) and re-weigh each panel
  Target corrosion rate = 0.45 - 0.85 mg/cm2
Calibrating & Standardizing Corrosive Conditions Within Cabinet

## Slide 14
Factors Affecting The
Corrosion Rate of Nickel Test Panels
New panels or panels stored for a long time may require 24-48 hours of CASS exposure before the weight loss per 22 hours stabilizes
Keep panels in an operating test chamber to avoid passivity
Passive panels can be HCl pickled and then CASS exposed until consistent weight loss is obtained
Round robin testing has discovered that the test has poor precision. Root cause is under investigation
Nickel weight loss too low:
  Increase the spray pressure to increase the collection rate to the high end of the accepted range (2mL/hr)
  Lower pH of the bulk salt solution to produce a pH of 3.1 in the collectors
  Nickel weight loss too high
  Use the opposite of the above recommendations

## Slide 15: The Corrodkote Accelerated Corrosion Test, ASTM B380
For decorative electrodeposited coatings
Nickel/chromium coatings
Copper/nickel/chromium coatings
Substrates:
  Steel
  Zinc Alloys
  Aluminum Alloys
  Plastics
  Others

## Slide 16: Overview of Corrodkote Test
Type & number of test specimens
Preparation of test specimens
Application of a slurry containing:
cupric nitrate
ferric chloride
ammonium chloride
Position of specimens during test
Conditions in humidity chamber
Test cycle
Period of test
Cleaning of testing specimens

## Slide 17: Corrodkote Exposure Chamber
Can use modified salt-spray cabinet
Standard specimen supports
Controlled temperature & humidity
  102°±2°F (38°±2°C)
  Relative humidity @ 80 - 90%
  No condensation on any of the test parts
Provision for air circulation

## Slide 18: Slurry Application
Apply Slurry with Clean Paint Brush
  Apply with circular motion
  Completely cover specimen
  Smooth out coating
Allow Specimens to Dry
  Room temperature
  Relative humidity <50%
  1 Hour before placing in humidity chamber
Cut Edges Protected by Coating
  Paint
  Wax
  Tape
Partially covered test panel shows swirling pattern obtained with brush

## Slide 19: Corrodkote Test Cycle
Cycle definitions:
  One cycle = continuous exposure up to 20 hours
  Continuous operation = humidity chamber closed, operation interrupted briefly for placement or removal of test specimens
Wash off slurry and apply fresh slurry for successive cycles
Time period & # of cycles determined by OEM
Typical corrosion site development options:
  4 hrs. salt spray
  24 hrs. @ 100% condensing humidity

## Slide 20: Russian Mud Test, ASTM B995
Test Chamber:
Any ASTM B117 type chamber capable of controlling conditions at 60+/-3°C and 23 +/-5% RH
Parts must not touch each other or chamber walls
No drippage from one part to another
Test Slurry:
Prepare a stock solution containing 57.5g CaCl2 per 94mL of water + 8 mL of 0.25N NaOH. The pH of this solution should be 9.5+/-0.5
  Shelf life = 1 month
Mix 3 g Kaolin per 5mL of stock solution to produce a slurry.
Measure the pH of the slurry (after dilution with an equal amount of Type IV DI water). pH should be 7.0+/-.5
  Shelf life of slurry = 12 hours

## Slide 21: Russian Mud Test, ASTM B995
Specimen Preparation:
Clean test specimens with 50/50 mixture of isopropyl alcohol and Type IV DI water
Apply 0.6 mL of test slurry using a pipet to produce a circular spot (do not manually manipulate/spread the slurry)
Produce at least 3 replicate spots separated by a minimum of 1cm in all directions
Exposure:
Place specimens into test chamber so that the slurry spot is horizontal
Test duration and inspection intervals are not specified by ASTM

## Slide 22: Russian Mud Test, ASTM B995
Specimen Evaluation:
At each inspection interval, wipe off the slurry and inspect using 10X magnification
Assign a rating at each spot per photos in ASTM B995-Appendix X1:
0 = complete or nearly complete loss of chromium
1 = 59+% chromium loss
2 = large localized chromium loss
3 = Slight chromium loss
4 = hazing or stain/no chromium attack
5 = no change
Rating “1”
Photo courtesy of Atotech

## Slide 23
Acetic Acid Salt Spray ASTM G85, Annex A1
Equipment:
  ASTM B117 cabinet
5% Salt solution
pH 3.1-3.3 (adjusted with acetic acid)
Cabinet temperature at 92-97ºF
Saturation tower temperature specified at 115-119ºF
Exposure angle 6-45º
Useful for investigating the effect of operational parameter changes in an electroplating process

## Slide 24: Kesternich Test (ASTM G87)
Overview:
Damp heat alternating atmosphere containing 0.2, 1.0 or 2.0 liters SO2 in a 300L (10.6ft3) test chamber
Exposure Options:
“A”: 1-24 Hr. continuous cycle
“B”: 8 Hrs. SO2 exposure at 40+/- 3°C (104°F) + 16 Hrs. at room temperature (cabinet open)
Highly suited for finding faults in surface coatings
Not suitable for comparing performance relationships between different coatings

## Slide 25: Kesternich Test
Cabinet:
Lead lined steel frame with glass walls
Pressure balanced with equalizing valves
Means of measuring/delivering prescribed volume of gas (as low as 0.2L) into the chamber (rotameter preferred)
Caution: Return of moist sulfur dioxide back into the cylinder can cause an explosion. Install check valve on line from cylinder to apparatus
Test Conditions:
Room atmosphere <75%RH
Protect from drafts/sunlight
Operate new cabinet for 10 cycles @ 2% SO2 before conducting a real test
Thermometer
Gas in
Water trough

## Slide 26: Kesternich Test
Test Specimen Exposure:
Introduce 2L distilled water into chamber
Place specimens at least 2cm apart, and at least 10cm from any wall or ceiling, at least 20cm above water in bottom of chamber
Angle of test surface is 0-10° from vertical
Introduce specified volume of gas
Heat chamber to 40+/-3°C in about 1.5 hours and then maintain temperature for duration of cycle

## Slide 27: The End, Thank You!